Technical data sheet:

Mohawk Via Linen: expressive colours and textures

Mohawk Via Linen has a subtle, embossed pattern. This understated, refined surface offers exceptional ink holdout and the ability to handle a wide range of specialty print processes making it the perfect paper solution for all creative and graphical communication projects.

- Specified by the US print and creative communities for over 25 years

- Delivering Mohawk quality and performance at a budget-friendly price point

- Manufactured acid free to meet ANSI standards for archival permanence

- Excellent on-press performance – uniform, stable and consistent

- Available with i-tone surface technology for HP Indigo printing

- Manufactured with wind energy, produced carbon neutral and FSC certified

| FINISH | SHADE | GSM | CALIPER [µ] | OPACITY | TAPPI | CIE | PPI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Linen | Pure White | 100 | 127 | 93 | 96 | 143 | 384 |
|  |  | 120 | 162.5 | 95 | 96 | 143 | 358 |
|  |  | 220 | 284.5 | 98.5 | 96 | 143 | 194 |
|  |  | 270 | 353 | 99 | 96 | 143 | 164 |
|  |  | 350 | 419 | 99 | 96 | 143 | 142 |
|  | Natural | 100 | 127 | 93 |  |  | 384 |
|  |  | 120 | 162.5 | 94 |  |  | 358 |
|  |  | 220 | 284.5 | 98 |  |  | 194 |
|  |  | 270 | 353 | 99 |  |  | 164 |
|  |  | 350 | 419 | 99 |  |  | 142 |